K5cable6        flexible Kapton cables and ground strap

Revision note: Cable width reduced from K5cable5 version

Drill information is the same.

Construction          Three layer board 18um copper layers -100um kapton between layers

Layup

C15stif             FR4 500um stiffener applied after construction

C15mskt	Photo imaged polyimide solder resist ?

C15m2		top layer metal plane

100um kapton

C15m3             Central metal traces. Note. There are no traces present on  the ground strap

100um kapton

C15m4	Bottom layer metal plane   N.B.  Surface mount connectors are mounted on the bottom side

C15mskb	Photo imaged polyimide solder resist ?

Finish 		As appropriate for SMD attach

Design rules 	Min track and gap 6thou 	minimum hole 12thou

In a 32 thou land

Land and pad to plane clearance 8 thou

Overall dimension of layout containing two cables and one ground strap –

approx		330mm x 160mm

Notes: 1) A metal 1 image is supplied but may not be needed depending on layup as all holes are under the stiffener – Via holes do not go through the stiffeners

2) Holes at the ends of the connectors are for placement and need to be drilled through the stiffeners.

3) Finished circuits can be supplied as individual pieces rather than as a

panel